Straw Wattle™

Specifications

UV-9 plastic net

The UV-9 Straw Wattles™ are manufactured from certified noxious weed free rice straw and are wrapped in a tubular UV degradable plastic netting.  They are nine inches in diameter (+/- one inch), 25 feet long (+/-0.5 feet), and have a density weight of approximately 1.8 pounds per foot (+/- 10%).

The netting has a strand thickness of 0.03 inch, a knot thickness of 0.055, a weight of 0.35 ounce per foot (each +/- 10%), and is made from 85% high density polyethylene, 14% ethyl vinyl acetate, with 1% color for UV inhibition.

The netting has a life expectancy of 3-5 years.